SCHOOL OF CHEMICAL, BIOLOGICAL & MATERIALS ENGINEERING

# and

# THE UNIVERSITY OF OKLAHOMA BIOENGINEERING CENTER

# The University of Oklahoma

# Norman, Oklahoma

2004 – 2005 Seminar Series

## CBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBME

#### DR. T. J. MOUNTZIARIS

#### PROFESSOR

#### DEPARTMENT OF CHEMICAL ENGINEERING

#### UNIVERSITY OF BUFFALO (SUNY)

#### BUFFALO, NEW YORK

#### AND

#### DIVISION OF CHEMICAL AND TRANSPORT SYSTEMS

#### NATIONAL SCIENCE FOUNDATION

#### ARLINGTON, VIRGINIA

##### Will present a seminar on

### “SYNTHESIS AND FUNCTIONALIZATION OF

### COMPOUND SEMICONDUCTOR NANOCRYSTALS”

Nanocrystals of compound semiconductors (e.g. CdSe, ZnSe, CdS, PbSe, etc.) that confine excitons (i.e., electron-hole pairs) in zero dimensions are attracting a lot of attention because of their unique size-dependent properties and their potential to revolutionize clinical diagnostics, photovoltaics, and high-density optoelectronics.

This presentation will focus on the synthesis and functionalization of ZnSe nanocrystals (quantum dots). Two new synthesis techniques have been developed in our laboratory that offer distinct advantages for large-scale production of these materials:

- Microemulsion-gas contacting: This technique exploits the dispersed phase of self-assembled

microemulsions to form numerous identical nanoreactors producing almost monodisperse

nanocrystal populations.

- Vapor-phase synthesis in a counterflow jet reactor: This technique is compatible with the

existing infrastructure of the microelectronics industry.

Surface passivation and functionalization protocols have been developed to exploit the size-dependent luminescence of the nanocrystals in novel multiplexed biosensors and DNA arrays. Studies of the fundamental links between transport phenomena, reaction kinetics, particle nucleation, cluster coalescence, and nanocrystal properties are being performed.  We employ a combination of experiments and multi-scale process models in order to identify optimal synthesis conditions. Recent extensions of this work in the synthesis of additional materials (e.g., CdSe) and templated growth of one-dimensional nanostructures (nanorods) in liquid crystals will also be discussed.

### THURSDAY, FEBRUARY 10, 2005

COOKIES AND COFFEE -- 2:30 P.M.

SEMINAR -- 3:00 P.M.

#### SARKEYS ENERGY CENTER, ROOM M-204

THIS IS A REQUIRED SEMINAR FOR CHE 5971