SCHOOL OF CHEMICAL, BIOLOGICAL & MATERIALS ENGINEERING

And

UNIVERSITY OF OKLAHOMA BIOENGINEERING CENTER

# The University of Oklahoma

# Norman, Oklahoma

2007 – 2008 Seminar Series

## CBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBMECBME

OUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBCOUBC

#### DR. CARSTEN SIEVERS

#### POSTDOCTORAL FELLOW

#### SCHOOL OF CHEMICAL AND BIOMOLECULAR ENGINEERING

#### GEORGIA INSTITUTE OF TECHNOLOGY

#### ATLANTA, GEORGIA

##### Will present a seminar on

### “LANTHANUM EXCHANGED ZEOLITES

### AS REFINING CATALYISTS”

Lanthanum exchanged faujasite type zeolites play an important role in modern refineries as catalysts for fluid catalytic cracking (FCC).  The lanthanum cations increase the hydrothermal stability of the zeolite and play a role in the formation of Brønsted acid sites during the preparation of the catalyst.

In addition to the application for FCC, lanthanum exchanged faujasite with a high aluminum content (LaX) is promising catalyst for isobutane/2-butene alkylation.  This process provides a mixture of isooctanes, which are ideal gasoline additives due to their high octane number.  Currently, HF and H2SO4 are used as alkylation catalysts in industrial plants.  Due to the handling hazards of these catalysts the transition to a solid acid catalyzed process is highly desirable.  However, premature catalyst deactivation by formation of carbonaceous deposits has prevented the use of solid alkylation catalysts, so far.  We have investigated the deactivation mechanism of LaX in isobutane/2-butene alkylation in detail.  Catalytic experiments were conducted for different times on stream and the spent catalysts were characterized by a variety of physicochemical techniques.  It was found that catalyst deactivation is caused by a combination of site poisoning and pore mouth plugging.  The carbonaceous deposits mainly consist of byclic compounds with alkyl side chains.  Based on these results suggestions for a suitable regeneration procedure are made.

### THURSDAY, JANUARY 10, 2008

COOKIES AND COFFEE -- 1:45 P.M.

SEMINAR -- 2:00 P.M.

#### SARKEYS ENERGY CENTER, ROOM M-204

THIS IS A REQUIRED SEMINAR FOR CHE 5971